## Slide 1
Singapore
25,000,000 tons/yr
Malaysia
200,000,000 tons /yr
Philippine
300,000,000 tons /yr
Thailand
400,000,000 tons /yr
Vietnam
500,000,000 tons /yr
Indonesia
500,000,000 tons /yr
1 Unit = 25,000,000 tons/yr
The following countries yearly consume 2,000,000,000 tons of construction materials, accounting for 200,000,000 tons of CO2 emission.

## Slide 2
Photo by Andrey Radchenko, from 500px.com
Harvesting sand, gravel and clay for construction materials leaves permanent marks on our landscape and cause long-term damage to our environment that may never recover.

## Slide 3
We develop a technology to lock CO2 in construction waste, and use it to replace a significant amount of normal cement, obtaining great strength.
42.5 MPa (standard strength at 28 days)
Replace 50% cement
Replace 30% cement

## Slide 4
Cl-
Sea water
Rebar and concrete
Cl- ingression profile
Corrosion threshold
normal concrete
Sustainable concrete
 | Chloride diffusion coefficient (m2·s-1)
OPC | 1.17×10-9
LC3 | 2.23×10-11
The waste-containing sustainable concrete provides 10 times better resistance to seawater corrosion.

## Slide 5
Calcite
Silica gel
We monitor the kinetics of carbonation process for more effective production.

## Slide 6
We circulate waste for all types of construction practices in Singapore.